ZX-C2-08

Oil-Gas Gathering and Transportation Corrosion Inhibitor - oil soluble

General 
Oil and gas gathering and transportation corrosion inhibitors ZX-C2-08 are widely used in the field of pipeline anti-corrosion in industries such as petroleum, natural gas, and urban gas. In these industries, pipelines are important transportation channels. If corrosion occurs inside the pipelines, it will lead to serious consequences such as pipeline damage, oil leakage and explosion. Therefore, it is of vital importance to use corrosion inhibitors to prevent corrosion of pipelines.

The content of corrosive media such as CO2, H2S, and CI - in the produced fluid from oil and gas Wells is relatively high, causing severe corrosion to casing and tubing. Oil and gas gathering and transportation corrosion inhibitors ZX-C2-08 is a liquid oil-soluble corrosion inhibitor compounded from components such as oleate imidazoline, dialkyl imidazoline, polyol phosphate ester, and surfactant. 

It has the advantages of high corrosion inhibition rate, low freezing point, good dispersibility, good thermal stability and low toxicity. It can quickly form a dense and firm protective film on the metal surface and has strong corrosion inhibition performance against various corrosive factors. This product has good compatibility with other downhole agents.

Composition




oleate imidazoline, dialkyl imidazoline, polyol phosphate ester, and surfactant.

Product properties
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Appearance                           Light yellow to Reddish brown liquid

Density                               0.9 - 1.0 (g/cm3, 20℃)

Solubility							   	Dispersed in water, soluble in diesel, kerosene 											and aromatic hydrocarbons

Freezing point                         <= -20 ℃ in winter, no data in summer

PH (100% pure, not deliuted)            5.0 - 9.0

Corrosion rate                          ＞80%

Application



[bookmark: _GoBack]Working Principle

When Oil and gas gathering and transportation corrosion inhibitors ZX-C2-08 is used for the first time, it should be pre-film first. 
The injection can be carried out in either continuous or intermittent manner. 
For sulfur-containing production gas Wells (without separators), it is recommended to inject gas through the casing loop and return it through the tubing to form a certain circulation system. For frequently closed gas Wells, it is recommended to add oil and casing respectively. For oil and gas gathering and transportation pipelines, direct refueling is possible。

Calculation method for pre-film dosage
1. Pre-film area: calculated as the inner and outer surface areas of the gas well tubing + the inner surface area of the casing + the inner surface area of the ground pipeline to be protected;
2. Pre-film thickness: 75μm.

It is recommended that gas Wells be injected periodically and intermittently, with a recommended dosing cycle of 30 days.

It is recommended to continuously add chemicals to the oil well. The recommended dosage is calculated based on the produced liquid, and the recommended concentration is 30-50 PPM

Storage 

Transportation: It should be avoided to be transported together with corrosive substances and pointed items.

Storage: Keep in a dry and well-ventilated warehouse. Avoid storing with corrosive substances. Shelf life: 2 years

Packing
Packaging: 200L or IBC ton drum plastic drum packaging.

Safety and handling 


Skin and eye contact: Rinse immediately with plenty of water.
Accidental ingestion: Drink plenty of warm water, induce vomiting, and seek medical attention.
Operation protection: Wear PVC, PE or rubber gloves.
Leakage: Rinse with plenty of clean water
